Anti Micropitting Gear Oil

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servomesh Plus 100 Servomesh Plus 150 Servomesh Plus 220 Servomesh Plus 320 Servomesh Plus 460 Servomesh Plus 680 Servomesh Plus 1000 | 90 – 110 135 – 165 198 – 242 288 – 352 414 – 506 612 – 748 900 - 1100 | 90 90 90 90 90 90 80 | 204 204 232 232 232 232 280 | Servomesh Plus Oils are advanced extreme pressure type industrial gear lubricants specially formulated to protect heavily loaded gears against micropitting. They meet performance requirement of Flender AG, AGMA 9005-D95, US Steel 224, DIN 51517 CLP, David Brown S1.53.101, SEB 181-226. They provide extended component life, excellent wear protection and improved protection from micropitting fatigue. |