Foodgrade Chain Lubricants

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servochainlube FG 150 Servochainlube FG 220 | 135 – 165 200 - 240 | 149 151 | 230 230 | Servochainlube FG Oils are specially designed, fully synthetic anti-wear chain oils for lubrication of drive and transport change in the food processing industry. Blended from selected synthetic fluids and additives, they are listed by National Sanitary Foundation (NSF), USA as category H1 Lubricant for use where there is potential of incidental food contact. |