Foodgrade Hydraulic Oils

| PRODUCT | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servosystem FG 32 Servosystem FG 46 Servosystem FG 68 | 29 – 35 42 – 50 62 - 74 | 135 130 130 | 210 220 220 | Servosystem FG Oils are specially designed synthetic hydraulic fluids for Food Processing Industry. They are formulated with selected synthetic hydrocarbon base oil and additives and are listed by National Sanitary Foundation (NSF), USA as H1 category food grade lubricants. |