Hydraulic-cum-Machine Tool Way Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servoway H 32 Servoway H 57 Servoway H 68 Servoway H 68 BD | 29 – 35 54 – 60 62 – 74 64 - 72 | 90 90 90 90 | 194 198 200 200 | Servoway H oils are combined hydraulic and machine way lubricants. These oils possess adequate lubricity to eliminate stick-slip and chatter under moderate load conditions and at the same time serve as hydraulic media in non-critical systems. Servoway H 32 meets ASLE standard W 150 and Cincinnati Milacron specification P-53. These oils are exclusively recommended for machine tools, which have combined hydraulic and way lubrication systems. Servoway H oils are not recommended for critical hydraulic systems or as a substitute for Servoway oils. Servoway H 68 BD exceeds the Indian requirement of minimum 70% biodegradability for ECO MARK. |