Oil Mist Lubricants

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servomist Lube 220 Servomist Lube 460 | 210 – 230 425 - 500 | 90 90 | 232 232 | Servomist Lubes are premium quality oil mist lubricants with excellent film strength, and thermal-oxidation stability characteristics. They are designed to exhibit good misting properties as required in oil mist lubricant systems for industrial gear applications. |