### Pneumatic Tool Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Pour Point C, Max. | Flash Point COC, C, Min. | Description / Application |
| --- | --- | --- | --- | --- | --- |
| Servoneum 100 Servoneum 181 Servoneum 220 | 90 – 110 176 – 186 198 - 242 | 90 90 90 | (-) 9 (-) 9 (-) 9 | 194 200 230 | Servoneum oils have excellent load carrying ability and rust preventive properties Servoneum oils maintain oil protective films both at low and high pressure and do not give obnoxious odour even with equipment operating in confined spaces. These oils are used for lubrication of pneumatic equipment such as rock drill, jack hammers, chippers, wagon drills etc., and are also used in small in-plant pneumatic tools like grinders, filing tools, drills, tappers, impact wrenches etc. |