# GRADES AVAILABLE - SERVO 4T ZOOM

DESCRIPTION

Servo 4T Zoom is high performance engine oil for 4 stroke 2/3 wheelers.  This oil is a   high viscosity index, 4 stroke engine oil.

# APPLICATION

Servo 4T Zoom is recommended for new generation 4 stroke motorcycles, scooters and auto rickshaws.

# PERFORMANCE STANDARDS

- JASO T 903 : API SJ / JASO MA 2

# PERFORMANCE BENEFITS

- Maximum power output.

- Superior performance in terms of oxidation stability.

- Excellent wear protection at high temperatures and severe operating conditions.

- Outstanding overall engine cleanliness.

- Enhanced engine & gear life.

- Higher fuel efficiency.

- Potential oil drain period of more than 5000 Kms.

# CHARACTERISTICS

| #### SAE GRADE | ##### 20W-40 |
| --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 13.5 – 15.5 |
| Viscosity Index, Min. | 110 |
| ## Flash Point, COC, ºC, Min | 200 |
| Pour Point, ºC, Max | (-) 21 |
| TBN, mg KOH/gm | 5.5 – 7.0 |