# GRADES AVAILABLE - SERVO GEAR SUPER 85W-140

DESCRIPTION

Servo Gear Super 85W-140 oil is an extreme pressure automotive gear lubricant. This oil is blended from selected base stocks and contain specific additive package to provide extreme pressure, anti-rust-corrosion characteristics.

# APPLICATION

Servo Gear Super 85W-140 oil is  recommended for passenger car, bus and highway truck hypoid, spiral bevel and worm gear axles and also manual transmission for which an extreme pressure gear lubricant of this type is required.

# PERFORMANCE STANDARDS

Servo Gear Super 85W-140 meets

- API Service GL 5

- US military MIL-L-2105

# PERFORMANCE BENEFITS

- Satisfy the lubrication requirements of a wide variety of gears.

- Provide protection against wear, due to good EP characteristics

- Give long service life even under high temperature operation since it has excellent oxidation stability.

- Provide good protection against corrosion.

# CHARACTERISTICS

| SAE GRADE | ##### 85W-140 |
| --- | --- |
| Kinematic Viscosity cSt @ 100C | 28 – 32 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), C Min. | 180 |
| Pour Point, C Max. | (-) 18 |