# GRADES AVAILABLE - SERVO GEAR SUPER 80W, 80, 85W, 80,  90, 140

DESCRIPTION

Servo Gear Super oils are automotive extreme pressure gear oils blended from specially selected high viscosity index base stocks and contain additives which impart extreme pressure, anti-rust, anti-corrosion and anti oxidation characteristics.  These are multi-purpose type gear lubricants specifically formulated to meet the rigorous service demand of commercial fleet mechanical transmissions, axles and gear boxes.

# APPLICATION

Servo Gear Super oils are primarily recommended for the lubrication of hypoid differential units operating under severe conditions and other types of mechanical transmissions and drive axles where extreme pressure gear oils are required.

# PERFORMANCE STANDARDS

Servo Gear Super oils meet the following specifications:

- API Service GL5

- US Military MIL-L-2105D

- UK Defence CS 3000B

- IS : 1118-1992

# APPROVALS

Servo Gear Super oils are approved by :

- Bharat Earth Movers Ltd., Bangalore

- Escorts J.C.B. Ltd., Faridabad

- Hindustan Motors Ltd., Trivellore

# PERFORMANCE BENEFITS

Servo Gear Super oils

- Have exceptional chemical and thermal stability permitting use upto bulk oil temperature of 150C

- Have excellent extreme pressure property to give maximum protection against low speed-high torque wear and high speed – shock induced scoring

- Guard automotive gear assemblies against rust and corrosion

# CHARACTERISTICS

| SAE GRADE | 80W | 80 | 85W | 85 | 90 | 140 |
| --- | --- | --- | --- | --- | --- | --- |
| Kinematic Vis. cSt @ 100C | 8 – 10 | 9 – 11 | 11 – 12 | 11.5 – 13 | 16 – 18 | 28 – 34 |
| Viscosity Index, Min. | 90 | 90 | 90 | 90 | 90 | 90 |
| Flash point (COC), C Min. | 165 | 180 | 180 | 180 | 180 | 180 |
| Pour Point, C Max. | (-) 27 | (-) 6 | (-) 9 | (-) 6 | (-) 9 | 0 |