# GRADES AVAILABLE - SERVO SUPER MG 5W-30/10W-30/10W-40/20W-40/20W-50

DESCRIPTION

Servo Super Multigrade Oils are blended from highly refined base stocks and balanced additive package containing shear stable VI improver, metallic detergent dispersant and anti-oxidant.  These oils are formulated to meet lubrication requirements of both gasoline and diesel engines.   Servo Super Multigrade Oils are red in colour and suitable for all seasons.

# APPLICATION

# Servo Super MG oils are recommended for

# Modern passenger cars

- Naturally aspirated diesel engines operating under severe conditions.

- Supercharged diesel engines

- Vehicles encountering continuous start-stop operation.

# PERFORMANCE STANDARDS

Meets the following specifications:

API SC/CC

US MIL-L-2104B

E-PL 1/E-DL 1 of  IS:13656-2002

# APPROVAL

Servo Super MG oils are approved by leading auto manufacturers like-

TELCO, Ashok Leyland , Mahindra & Mahindra, Bajaj Tempo, etc.

# PERFORMANCE BENEFITS

## Servo Super Multigrade Oils

- Enable easy low temperature starting

- Minimise fuel and oil consumption

- Give longer battery life

- Provide maximum protection to engine parts against rust and corrosion

- Give good high and low temperature performance in the engine

- Minimise wear of engine parts

- Ensure system cleanliness by holding contaminants in finely dispersed state

# CHARACTERISTICS

| SAE GRADE | 5W-30 | 10W-30 | 10W-40 | 20W-40 | 20W-50 |
| --- | --- | --- | --- | --- | --- |
| Kinematic Viscosity cSt @ 100C | 11-12 | 9.5 – 11.5 | 13.5 – 15.5 | 13.5 – 15.5 | 17.5 – 19.5 |
| Viscosity Index, Min. | 150 | 135 | 140 | 110 | 125 |
| Flash point (COC), C Min. | 160 | 190 | 190 | 200 | 200 |
| Pour Point, C Max. | (-) 33 | (-) 27 | (-) 27 | (-) 21 | (-) 21 |
| TBN, mg, KOH/gm | 9.2-12.0 | 6.5-8.5 | 4.5-6.0 | 4.2-8.0 | 4.5-6.0 |