# GRADES AVAILABLE – SERVO TRACTOR OIL 20W-40

DESCRIPTION

Servo Tractor Oil is Multigrade Universal Tractor Oil specifically formulated to meet all the lubrication requirements of tractors.    It has a high detergency level and excellent oxidation stability combined with good antiwear and antiweld properties.

# APPLICATION

Servo Tractor Oil is recommended for the engine, combined transmission, gear box and hydraulic system of all makes of tractors.

# PERFORMANCE STANDARDS

- API CD for engine oil and API GL 4 for gear oil

- US Military MIL-L-45199B for engine oil and MIL-L-2105 for gear oil

- E-DL2 of IS:13656-2002

- Caterpillar series 3

#### MANUFACTURERS APPROVAL

  - Tractor oil is recommended by leading tractor manufacturers.

# PERFORMANCE BENEFITS

- Excellent all weather performance.

- Prevents wrong use and mixing up of different oils in applications.

- Reduces the inventory of different grades.

- Extends oil and equipment life.

# CHARACTERISTICS

| #### SAE GRADE | ##### 20W-40 |
| --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 14.5 – 16.3 |
| Viscosity Index, Min | 110 |
| Flash Point, COC, ºC, Min | 200 |
| TBN mg KOH/gm | 9.5 – 11.5 |