GRADES AVAILABLE -  SERVO TRANSTRAC 30

DESCRIPTION

Servo Transtrac 30 is a Universal Tractor Transmission Oil (UTTO) developed to meet the   diverse performance requirements of farm tractor lubricants such as the controlled friction requirements of  power take off clutch and wet brakes, suppression of wet brake noise, good filterability and antifoam characteristics, protection against rust and corrosion and adequate EP and antiwear properties for maximum durability of the transmission, differential and final drive.

# APPLICATION

Servo Transtrac 30 is recommended for use as   Universal Tractor Transmission Oil and in powershift transmissions and torque converters in off-highway equipment.

# PERFORMANCE STANDARDS

Meets the following OEM service specification

# Tractor OEM

Ford New Holland 	- M2C 134 D

Massey Ferguson    - M1135 & M1141

John Deere	         - J 20 C, J 14 A, J 20 D

White Farm	         - Q 1826

# Transmission

Allison     -  C4

# Hydraulics

Denison    -    HF-0, HF-1, HF-2

# PERFORMANCE BENEFITS

- One oil can be used for hydraulics, transmission, wet brake, PTO and final drive in farm tractors thereby reducing inventory cost.

- Reduced lubricant misapplication by farmers.

- Outstanding thermo - oxidative stability resulting in longer fluid life.

- Enhanced protection against corrosion.

- Longer component life.

# CHARACTERISTICS

| #### GRADE | Transtrac 30 |
| --- | --- |
| Appearance | Clear |
| Kinematic Viscosity, cSt @ 100C | 10 – 10.5 |
| Flash Point COC, Deg C, Min. | 190 |
| Pour Point, Deg C, Max | (-) 30 |
| Viscosity Index, Min | 95 |
| TBN Mg, KOH/gm | 3.5 – 4.5 |