# SERVO 4T SYNTH 10W-30

DESCRIPTION

Servo 4T Synth 10W-30 is blended with structurally modified base stock blended with synergistic additive system for outstanding detergency, dispersancy characteristics, anti-wear and antioxidant properties, high viscosity index   and low temperature flow properties. This delicately balanced composition provides and exceeds tough industry performance standards thus ensuring reliability, emission control, economy and endurance.

# APPLICATION

Servo 4T Synth 10W-30 is recommended for on road high performance 4 Stroke Motor Cycle and Scooters particularly operating with wet clutch system.

# PERFORMANCE BENEFITS

- Selected synthetic base stocks impart inherent low temperature pumpability and excellent evaporation control in high speed, high temperature operation.

- Formulated with highly shear stable viscosity index modifiers which ensure viscosity control over extreme temperatures.

- Enhanced lubrication to help maintain maximum power and acceleration over the life of the engine.

- Optimized wet-clutch performance.

- Excellent low temperature flow characteristics to help minimize engine wear during start up.

- Potential improvement in fuel economy.

- Enhanced oil life and longer drain period.

SPECIFICATIONS

Servo 4T Synth 10W-30 meets the performance requirement of API SM /JASO MA 2 specifications.

# CHARACTERISTICS

| Kinematic Viscosity, cSt, @ 100C | 10 - 12 |
| --- | --- |
| Viscosity Index, Min | 150 |
| Flash Point (COC), C Min. | 200 |
| Pour Point, Deg C | (-) 30 |
| TBN, mg KOH/gm | 7.0 – 7.5 |
| Sulphated Ash, % wt | 0.80 – 0.85 |

Jul-26