SERVO XEE SJ

DESCRIPTION

Servo XEE SJ oils are long life, high performance fuel economy engine oil for new generation petrol and diesel vehicles.   These oils are blended from high viscosity index base stocks and contain additives to meet the highest quality performance standard

# APPLICATION

Servo XEE SJ oils are recommended for new generation imported and Indian passenger cars using petrol.

# PERFORMANCE STANDARDS

- API SJ in gasoline and API CF in diesel service.

- ACEA A3/B3 – 96, MB 229.1

- Fuel economy standards API EC II & EC I for 10W-30 and 10W-40 grade respectively.

# PERFORMANCE BENEFITS

- Superior performance in terms of improved oil and engine life.

- Less oil thickening, better deposit control.

- Excellent Engine Cleanliness.

- Catalytic Convertor Compatible.

# CHARACTERISTICS

| #### SAE GRADE | 10W-30 | 10W-40 | 15W-40 | 20W-50 |
| --- | --- | --- | --- | --- |
| Kin.Viscosity @ 100ºC, cSt | 9.5 – 11.0 | 13.5 – 14.5 | 13.5 - 14.5 | 17.5 – 19.5 |
| Viscosity Index, Min | 130 | 140 | 130 | 130 |
| Flash Point, COC, ºC, Min | 200 | 206 | 206 | 206 |
| Pour Point, C, Min. | (-) 30 | (-) 27 | (-) 24 | (-) 21 |
| TBN, mg KOH/gm | 9 – 11 | 9 – 11 | 9 – 11 | 9 - 11 |

Jul-26