Special Purpose High VI Hydraulic Oil (Anti-wear Type)

| PRODUCT | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servosystem HVLP 22 Servosystem HVLP 46 Servosystem HVLP 68 | 20 - 24 42 – 50 62 - 74 | 140 165 150 | 165 204 200 | Servosystem HVLP Oils are all-weather high anti-wear hydraulic oils formulated with superior quality hydro treated base stocks. They have very high viscosity index, very low pour point and excellent low temperature fluidity for use in equipments working at high altitudes and under wide ambient temperature variation. They meet DIN 51524 Part 3 specifications. |
| Servohydrex 15 Servohydrex 32 Servohydrex TH 46 Servohydrex 68 Servohydrex 100 | 13 – 17 29 – 33 43 – 48 65 – 72 100 – 110 | 150 160 135 145 130 | 150 140 200 200 220 | Servohydrex oils are very high viscosity index, anti-wear type hydraulic oils which possess excellent lubrication characteristics. These oils are recommended for very low operating temperature conditions. Servohydrex TH 46 is recommended for Tata Hitachi excavators and Servohydrex 100 is approved by L&T for use in Poclain excavators. |