Synthetic Chain Lubricants

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servochainlube S 135 Servochainlube S 220 | 130 – 145 198 – 242 | 105 100 | 290 300 | Servochainlube S Oils are specially formulated synthetic product for lubrication of bearings, chains, slides and gears in industrial applications where air temperature often exceeds 260 deg C. They are suitable for use in ceramic paint, fiber glass plants, foundries steel mills, automotives plants, paper, rubber, textile industry etc. |