Vacuum Pump Oil

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Pour Point C, Max. | Flash Point COC, C, Min. | Description / Application |
| --- | --- | --- | --- | --- | --- |
| Servovacuum VM 4 | 47 – 58 @ 50C | 95 | (-) 15 | 230 | Servovacuum VM 4 is a specially developed product having low vapour pressure (1 x 10-6 mm of Hg at 200C) and high thermal stability. It meets GOST: 23013-78 specification for vacuum pumps oil and is recommended for high vacuum producing diffusion pumps. |