# GRADES AVAILABLE - SERVO BRAKE FLUID SUPER HD

DESCRIPTION

Servo Brake Fluid Super HD is heavy duty hydraulic brake fluid which ensures long service life of the brake fluid and components of brake mechanism. It remains clear and uniform fluid under extreme cold climatic conditions, enabling satisfactory operation of brake systems.

It is fully compatible with rubber seals used in Hydraulic Brake Systems.   It also lubricates the moving parts of the brake system very effectively.

# APPLICATION

Servo  Brake Fluid Super HD is designed for use in modem brake system of automotive vehicles operating in heavy duty conditions  The higher boiling point of this product provided greater safety factor while driving at high speed with heavy load or in hilly areas where frequent  braking generates higher temperatures in the brake system.

Servo Brake Fluid Super HD is recommended for various hydraulic brake systems including disc type.

# PERFORMANCE STANDARDS

Servo Brake Fluid Super HD meets the following specification:

- SAE J 1703

- FMVSS 116.3 DOT 3

- IS:8654-1986

MANUFACTURERS APPROVAL

Servo Brake Fluid Super HD is approved by  TELCO, Maruti, Daewoo Motors, etc.

# PERFORMANCE BENEFITS

Servo Brake Fluid Super HD

- Provides very high safety factor during driving at high speed in city and under heavy load in hilly regions

- Provides excellent protection against corrosion to iron, non-ferrous metals and zinc alloys

- Has longer service life, due to excellent oxidation stability

# CHARACTERISTICS

| Appearance | Clear Homogeneous red liquid |
| --- | --- |
| Equilibrium Reflex Boiling Point, C Min. | 205 |
| Kinematic Viscosity, cSt @ (-) 40 C, Max. @ 100  C, Min. | 1500 1.5 |
| pH Value | 7.0-11.5 |