Open Gear Compound

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servocoat 110 Servocoat 120 Servocoat 140 Servocoat 170 Servocoat 170 T Servocoat 190 | 80 – 120 200 – 250 400 – 550 710 – 760 740 – 810 900 - 1100 | - - - - - - | 250 250 280 280 280 280 | Servocoat are open gear compounds having good load carrying ability and are recommended for open gear, wire rope and chain drive lubrication. Servocoat compounds are also for the lubrication of kiln tyres operating at high temperature in cement mills and chemical plants. These compounds should not be used in food processing industries. Servocoat 170 T has special tackiness additive and has been developed specifically to meet the requirements of Indian Railways. |