# GRADES AVAILABLE - -SERVO SUPERIOR 30, 40, 50 (SJ)

# CHARACTERISTICS

| SAE GRADE | 30 | 40 | 50 |
| --- | --- | --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 10.0 – 12.0 | 13.0 – 15.0 | 18.0 – 20.0 |
| Flash Point, COC, ºC, Min | 220 | 226 | 230 |
| Pour Point, ºC, Max | Minus 6 | Minus 6 | Minus 6 |
| TBN, mg KOH/gm | 5.0 – 7.0 | 5.0 – 7.0 | 5.0 – 7.0 |

# Text boxes

# APPLICATION

Servo Superior oils are recommended for new generation petrol and diesel cars. These oils are also suitable for existing passenger cars and four stroke two whellers i.e. scooters and motorcycles.

DESCRIPTION

Servo Superior oils are high performance engine oil for new generation petrol and diesel vehicles.   These oils are blended from high viscosity index base stocks and contain additives to meet the stated performance standards.

# PERFORMANCE BENEFITS

- Superior performance in terms of oxidation stability, dispersancy characteristics and energy efficiency.

- Excellent sludge control and extra wear protection at high temperatures and severe operating conditions.

- Outstanding overall engine cleanliness and also provide long engine life.

- Fuel savings and low oil top up.

- Catalytic Converter Compatible.

# PERFORMANCE STANDARDS

- API SJ in gasolene service.