##### SERVO BOAT POWER PLUS

DESCRIPTION

Servo Boat Power Plus is low smoke semi-synthetic two stroke engine oil developed to meet the critical requirements of high performance water cooled two stroke engines manufactured by leading engine makers.   It is blended from selected base stocks and additives to minimise spark plug fouling and preignition, prevent rusting, minimise deposit formation and provide protection against seizure, scuffing and wear.  It contains a diluent for easy mixing with gasoline.

# APPLICATION

Servo Boat Power Plus is recommended for lubrication of outboard motors operating on two stroke engines.

# PERFORMANCE STANDARDS

Meets

- NMMA TC-W3 specifications.

# PERFORMANCE BENEFITS

- Low exhaust smoke

- Maintains engine cleanliness

- Minimizes spark plug fouling

- Reduces port deposits and ring sticking

- Prevents seizure and scuffing

- Is easily pumpable by oil injection system

# CHARACTERISTICS

| ## Appearance | Clear |
| --- | --- |
| ## Kinematic Viscosity @ 40C, cSt | 42-60 |
| ## Flash Point (PMCC), C, Min | 90 |
| ## Pour Point, C, Max | (-) 30 |
| ## Sulphated ash % wt., Max | 0.05 |

Mar-11