GRADES AVAILABLE – SERVO CALIB 2, 5

DESCRIPTION

Servo Calib oils are low viscosity products specially developed as Calibration fluids for Diesel Injection equipments.

# APPLICATION

Servo Calib oils are recommended for calibration of Diesel Injectors.

# PERFORMANCE BENEFITS

- Increases the life of calibration equipment.

- Excellent seal compatibility

- Excellent oxidation stability property

- Excellent high temperature performance

- Excellent wear protection

- Excellent low temperature characteristics

# PERFORMANCE STANDARDS

Servo Calib 2 meets the specification requirement of ISO : 4113.

Servo Calib 5 has been specially developed for Diesel Injector equipments used by Indian Railways.

# CHARACTERISTICS

| #### GRADE | Servo Calib 2 | Servo Calib 5 |
| --- | --- | --- |
| Kinematic Viscosity cSt @ 40C | 2.45 – 2.75 | 5.2 – 6.2 |
| Density, gm/ml @ 29.5 Deg C | 0.826 | 0.835 |
| Pour Point, C, Max | (-) 10 | 0 |
| Flash Point, PMCC, C, Min | 75 | 130 |