SERVO FUTURA D

DESCRIPTION

Servo Futura D oil is a long life, high performance diesel engine oil compatible for engines conforming to advance emission norms.  This oil is highly refined high viscosity index base stocks and contain additives to meet the highest performance standard for Diesel Engines.

# APPLICATION

Servo Futura D oil is recommended for new generation diesel vehicles confirming to advanced emission norms. This oil is also recommended for new generation petrol vehicles.

# PERFORMANCE STANDARDS

- Meets API CI-4 requirement for diesel engine and API SL requirement for petrol engine.

- Meets MB 228.3 and Volvo VDS3 and Cummins CES 20076/20077/20078 ACEA E7 requirement.

# PERFORMANCE BENEFITS

- Increased component life.

- Lower maintenance costs.

- Excellent Engine Cleanliness.

- Excellent control on soot induced oil thickening.

- Outstanding control on oil consumption.

- Ensures outstanding protection from wear, high temperature deposits, oil degradation and corrosion.

- Suitable for vehicles fitted with EGR system.

# CHARACTERISTICS

| #### SAE GRADE | 15W-40 |
| --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 14 - 15 |
| Viscosity Index, Min | 135 |
| Flash Point, COC, ºC, Min | 200 |
| Pour Point, C, Min. | (-) 24 |
| TBN, mg KOH/gm | 9 – 12.5 |
| Sulphated Ash % wt | 1.23 – 1.64 |

Jul-26