SERVO FUTURA P  10W-30

DESCRIPTION

Servo Futura P oil is a premium performance petrol engine oil.  It is formulated with superior quality, high viscosity index base stocks and fortified with shear stable VI improvers. This and the performance additive system incorporated provide a fine balance of low temperature operatability and reduced volatility in running conditions. The formulation is optimised with phosphorous chemistry which ensures catalytic converter compatibility.

# APPLICATION

Servo Futura P oil is recommended for new generation petrol vehicles requiring highest performance levels.  Meets the requirement of advanced emission norms.

# PERFORMANCE STANDARDS

- Meets API SM for petrol engines.

- Meets ILSAC GF-4 performance in SAE 10W-30 viscometrics.

# PERFORMANCE BENEFITS

- Enhanced engine life.

- Reduced component wear.

- Fuel saving.

- Outstanding control on oil consumption.

- Meets advanced emission norms.

- Catalytic converter compatible.

# CHARACTERISTICS

| #### SAE GRADE | 10W-30 |
| --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 10 – 12 |
| Viscosity Index, Min | 130 |
| Flash Point, COC, ºC, Min | 190 |
| Pour Point, C, Min. | (-) 27 |
| TBN, mg KOH/gm | 7 – 8.5 |
| Sulphated Ash % wt | 0.75 – 0.92 |

Jul-26