# SERVOGREASE MP, MP 3

DESCRIPTION

Servo Grease MP & MP 3 are premium quality lithium soap, multi-purpose automotive grease, with high drop point, good thermal and structural stability and also having resistance against water wash out.  With smooth structure and high degree of resistance against oxidation and rusting/corrosion.   They are ideal product for all grease lubricated parts of automotive equipment.

# APPLICATION

Servo Grease MP is recommended for water pump, wheel bearings, chassis fittings and universal joints, including those of constant velocity type, for mobile equipment e.g., automotive, off- highway equipment such as tractors, construction equipment etc.   Servo Grease MP 3 is used as Wheel Bearing Grease in Automotive applications.

# PERFORMANCE STANDARDS

Servo Grease MP meets IS:12203:1987 (Reaffirmed 1993)

# MANUFACTURER’S APPROVAL

Servo Grease MP is approved by the leading manufacturers, such as :

- Bharat Earth Movers Ltd., Bangalore

- Escorts Ltd. (Tractor Division), Faridabad

- Hindustan Machine Tools, (Tractor Division), Pinjore

# PERFORMANCE BENEFITS

- Provide excellent resistance to structural and consistency changes, over wide range of temperatures but remains in place despite severe working or sustained shock impact

- Have excellent low and high temperature properties. Servo Grease MP can be dispensed at low temperatures and will maintain adequate stay-put property at the higher temperatures encountered in service

- Resist effectively, water wash out in use, assuring adequate lubrication over extended service periods

- Provide resistance to oxidation, rust and corrosion.

# CHARACTERISTICS

| ##### GRADE | Grease MP | Grease MP 3 |
| --- | --- | --- |
| NLGI Consistency | 2 | 3 |
| Colour | Brown | Brown |
| Structure | Smooth | Smooth |
| Soap Type | Lithium | Lithium |
| Worked Penetration, @25C, (60 Strokes) | 250 - 280 | 220-250 |
| Drop Point, C Min. | 180 | 180 |

Mar-11