Spindle Oils

| PRODUCT | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servospin 2 Servospin 5 Servospin 10 Servospin 12 Servospin 22 | 2.0 – 2.5 4 – 5 9 – 11 11 – 14 20 – 24 | - - - 90 90 | 70 70 144 144 160 | Servospin oils are recommended for bearing lubrication of high speed textile spindles and machine tool spindles. Other applications include timing gears, positive displacement blowers and tracer mechanism and hydraulic systems of precision machine tools. Servospin 10 meets IS: 493 Part 2 (Reaffirmed 1993). |
| Servospin EE 10 Servospin EE 22 | 9 – 11 20 –24 | 90 90 | 144 160 | Servospin EE oils are premium textile machinery oils developed specifically as energy efficient spindle lubricant for the ring frames. Formulated with superior quality hydro treated base stocks these oils offer improved service life and possess superior oxidation/thermal stability. These oils have potential of about 5% power saving. Approved by M/s. Kunal Engineering, LMW etc. |